# Void Fraction Ratio Calculation — Campaign C-104

# Objective

Determine the void fraction ε of Product 1 and Product 2 for Campaign C-104 using a droplet-to-particle shrinkage mass balance, and report the ratio ε₂/ε₁. The void fraction is the fraction of final particle volume that is empty after solvent removal.

# 1. Data filtering

Only RUN-mode records from dataset_1_production_history.csv (Campaign C-104) and PASS-status measurements from dataset_2_particle_size_qc.csv (Campaign C-104) are used. Records are matched by timestamp, keeping only timestamps where the Monitoring Port, Product 1, and Product 2 particle-size measurements all coincide with valid RUN-mode feed data. Across Campaign C-104 every RUN-mode feed record and every PASS particle-size record is identical, so all matched timestamps reduce to a single representative case.

# 2. Choice of particle-size statistic

dataset_2_particle_size_qc.csv reports d₁₀, d₅₀, d₉₀, span, and the volume mean diameter (D[4,3]) for every sample. Because this calculation is a mass (volume) balance between the droplet and the final particle, the diameter used must represent the volume-weighted population, not the count-median. d₅₀ is a number-based median and under-weights the larger droplets/particles that carry most of the volume, so the volume mean diameter is used consistently for the Monitoring Port, Product 1, and Product 2 diameters below.

# 3. Void fraction model

ε = 1 − xp · (ρd / ρp) · (Dd / Dp)3

where:

ε = particle void fraction

xp polymer mass fraction in the dispersed phase

ρd dispersed-phase density (g/cm³)

ρp polymer density = 1.34 g/cm³

Dd Monitoring Port (droplet) volume mean diameter

Dp final particle volume mean diameter (Product 1 or Product 2)

# 4. Polymer mass fraction

xp = Polymer A feed / (Polymer A feed + Solvent A feed) = 20.0 / (20.0 + 980.0) = 0.0200

# 5. Dispersed-phase density (ideal volume additivity)

1 / ρd = xp / ρp + (1 − xp) / ρs, with ρp = 1.34 g/cm³ and ρs = 1.33 g/cm³

ρd = 1.3302 g/cm³

# 6. Matched diameters (Campaign C-104)

Monitoring Port volume mean diameter, Dₔ = 80.0 µm

Product 1 volume mean diameter, Dₚ₁ = 30.0 µm

Product 2 volume mean diameter, Dₚ₂ = 25.0 µm

# 7. Void fraction results

ε₁ = 1 − (0.0200)(1.3302/1.34)(80.0/30.0)³ = 0.6235

ε₂ = 1 − (0.0200)(1.3302/1.34)(80.0/25.0)³ = 0.3494

Void fraction ratio (Product 2 : Product 1) = ε₂ / ε₁ = 0.3494 / 0.6235 = 0.5604

# 8. Consistency with solvent recovery data

Product 2 has a lower mean void fraction than Product 1 (denser particles with less retained internal volume), yet dataset3_evaporator_recovery_qc_report.pdf reports a higher loss-on-drying for the Product 2 line (0.12 wt%) than for the Product 1 line (0.10 wt%). The two figures are therefore not consistent with each other: a lower void fraction would normally be expected to correspond to less retained solvent, not more, so Product 2's higher loss-on-drying cannot be explained by its particle void fraction alone.