Summary of Adsorption Data at pH 3 and 9

Adsorption Data at pH 3

| Time (Min.) | Initial Abs. (a.u.) | Initial Con (Mol/L) | Abs. @ time T (a.u.) | Conc. @ time T (Mol/L) | Adsorption Capacity (Mol/g) | Adsorption Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 1.0916 | 136.4 | 1.0916 | 136.4 | 0.00 | 0 |
| 1 | 1.0916 | 136.4 | 1.0916 | 136.4 | 0.00 | 0 |
| 3 | 1.0916 | 136.4 | 1.0912 | 136.4 | 0.05 | 0 |
| 5 | 1.0916 | 136.4 | 1.0809 | 135.1 | 1.61 | 1 |
| 7 | 1.0916 | 136.4 | 1.0776 | 134.7 | 2.09 | 1 |
| 10 | 1.0916 | 136.4 | 1.0803 | 135 | 1.68 | 1 |
| 15 | 1.0916 | 136.4 | 1.0757 | 134.5 | 2.38 | 1 |
| 20 | 1.0916 | 136.4 | 1.0608 | 132.6 | 4.62 | 3 |
| 30 | 1.0916 | 136.4 | 1.0547 | 131.8 | 5.53 | 3 |
| 40 | 1.0916 | 136.4 | 1.0284 | 128.6 | 9.47 | 6 |
| 50 | 1.0916 | 136.4 | 1.0177 | 127.2 | 11.09 | 7 |
| 60 | 1.0916 | 136.4 | 0.9896 | 123.7 | 15.29 | 9 |
| 80 | 1.0916 | 136.4 | 0.9860 | 123.3 | 15.83 | 10 |
| 100 | 1.0916 | 136.4 | 0.9425 | 117.8 | 22.36 | 14 |
| 120 | 1.0916 | 136.4 | 0.9057 | 113.2 | 27.88 | 17 |
| 140 | 1.0916 | 136.4 | 0.8845 | 110.6 | 31.06 | 19 |
| 180 | 1.0916 | 136.4 | 0.8644 | 108.1 | 34.07 | 21 |
| 230 | 1.0916 | 136.4 | 0.8380 | 104.7 | 38.04 | 23 |
| 290 | 1.0916 | 136.4 | 0.8033 | 100.4 | 43.23 | 26 |
| 340 | 1.0916 | 136.4 | 0.7700 | 96.25 | 48.23 | 29 |
| 400 | 1.0916 | 136.4 | 0.7296 | 91.2 | 54.30 | 33 |
| 460 | 1.0916 | 136.4 | 0.7079 | 88.49 | 57.54 | 35 |

Adsorption Data at pH 9

| Time (Min.) | Initial Abs. (a.u.) | Initial Con (Mol/L) | Abs. @ time T (a.u.) | Conc. @ time T (Mol/L) | Adsorption Capacity (Mol/g) | Adsorption Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | 1.1454 | 143.2 | 1.1454 | 143.2 | 0.00 | 0 |
| 1 | 1.1454 | 143.2 | 1.1454 | 143.2 | 0.00 | 0 |
| 3 | 1.1454 | 143.2 | 1.1455 | 143.2 | 0.00* | 0 |
| 5 | 1.1454 | 143.2 | 1.1354 | 141.9 | 1.50 | 1 |
| 7 | 1.1454 | 143.2 | 1.1326 | 141.6 | 1.93 | 1 |
| 10 | 1.1454 | 143.2 | 1.1263 | 140.8 | 2.87 | 2 |
| 15 | 1.1454 | 143.2 | 1.1283 | 141 | 2.58 | 1 |
| 20 | 1.1454 | 143.2 | 1.1315 | 141.4 | 2.09 | 1 |
| 30 | 1.1454 | 143.2 | 1.1149 | 139.4 | 4.58 | 3 |
| 40 | 1.1454 | 143.2 | 1.1070 | 138.4 | 5.76 | 3 |
| 50 | 1.1454 | 143.2 | 1.0924 | 136.5 | 7.96 | 5 |
| 60 | 1.1454 | 143.2 | 1.0933 | 136.7 | 7.81 | 5 |
| 80 | 1.1454 | 143.2 | 1.0771 | 134.6 | 10.25 | 6 |
| 100 | 1.1454 | 143.2 | 1.0731 | 134.1 | 10.84 | 6 |
| 120 | 1.1454 | 143.2 | 1.0514 | 131.4 | 14.10 | 8 |
| 140 | 1.1454 | 143.2 | 1.0391 | 129.9 | 15.94 | 9 |
| 180 | 1.1454 | 143.2 | 1.0202 | 127.5 | 18.78 | 11 |
| 230 | 1.1454 | 143.2 | 1.0011 | 125.1 | 21.64 | 13 |
| 290 | 1.1454 | 143.2 | 0.9802 | 122.5 | 24.79 | 14 |
| 340 | 1.1454 | 143.2 | 0.9422 | 117.8 | 30.48 | 18 |
| 400 | 1.1454 | 143.2 | 0.9165 | 114.6 | 34.33 | 20 |
| 460 | 1.1454 | 143.2 | 0.8790 | 109.9 | 39.96 | 23 |

* Timestamp 3 (pH 9) computed to a slightly negative uptake from raw absorbance, within the instrument's noise floor; reported here as 0.00 mol/g / 0% rather than the negative artifact.

Analysis

For both pH conditions, adsorption capacity and efficiency increased steadily with contact time. Uptake was faster at pH 3, reaching about 10% adsorption efficiency after 80 minutes versus about 6% at pH 9. Over the full run, pH 3 reached an overall adsorption efficiency of 35% versus 23% at pH 9, and adsorption capacity rose from 0 to 57.54 Mol/g at pH 3 versus 0 to 39.96 Mol/g at pH 9, showing that adsorption is favored at pH 3.

Key Findings

Adsorption at pH 3 outperformed pH 9 on both capacity (57.54 vs 39.96 Mol/g) and efficiency (35% vs 23%).

Uptake was faster at pH 3, reaching about 10% efficiency by 80 minutes versus about 6% at pH 9.

Both conditions rose steadily with time and had not fully levelled off by 460 minutes.

Side-by-side comparison

| Parameter | pH 3 | pH 9 | Preferred |
| --- | --- | --- | --- |
| Adsorption capacity (Mol/g) | 57.54 | 39.96 | pH 3 |
| Adsorption efficiency (%) | 35 | 23 | pH 3 |